## Slide 1
RIE-Cl Trend Chart
July - 2018

## Slide 2: RIE-Cl Trend Chart - July 2018
Started from Nov 2017. patterned with AZ5214E resist, Dektak Measurement is done.
GaN Etch Rate ~ 55 nm/min
Chart: RIE-Cl_GaN Etch Rate
| 43131 | 43153 | 43186 | 43244 | 43280 | 43297
Upper Limit | 60.5 | 60.5 | 60.5 | 60.5 | 60.5 | 60.5
Lower Limit | 49.5 | 49.5 | 49.5 | 49.5 | 49.5 | 49.5
Target | 55 | 55 | 55 | 55 | 55 | 55
Average Etch rate (nm/min) | 55 | 55 | 55 | 55 | 55.87 | 55

## Slide 3: RIE-Cl Trend Chart - July 2018
SiO2 recipe used for tool monitoring
These recipes vary with respect to tool’s condition
Etch Rate of SiO2 is ~ 164 nm/min
Chart: RIE-Cl_SiO2 Etch Rate
| 43129 | 43153 | 43182 | 43207 | 43217 | 43251 | 43268 | 43297
Upper Limit | 187 | 187 | 187 | 187 | 187 | 187 | 187 | 187
Average Etch rate (nm/min) | 164.976 | 169.67 | 165.608 | 173.774 | 173.138 | 164.44 | 162.082 | 154.926
Lower Limit | 153 | 153 | 153 | 153 | 153 | 153 | 153 | 153
Target | 170 | 170 | 170 | 170 | 170 | 170 | 170 | 170